**آزمون­های تخصصی پوشش های خطوط لوله­های مورد استفاده در صنایع نفت، گاز و آب**

|  |
| --- |
| ***Epoxy Powder*** |
| ***ISO 21809-1*** | Density | 1 |
| ***ISO 21809-1*** | Gel time @ 200 °C | 2 |
| ***ISO 21809-2*** | Particle size | 3 |
| ***ISO 21809-1*** | Moisture content, max % | 4 |
| ***ISO 21809-1*** | Glass transition temperatureTg1Tg2**∆H** | 5 |
| ***ISO 21809-2*** | Cathodic Disbonding 28 Days 65 °C, 1.5 V | 6 |
| ***ISO 21809-2*** | 3.0° ppd flexibility, at -30 °C | 7 |
| ***ISO 21809-2*** | Hot Water Adhesion 24 hr At 75±3 °C | 8 |
| ***Adhesive*** |
| ***ISO 1183*** | Density @ 23±2 °C gr/cm3 | 9 |
| ***ISO 3146*** | Melting index (2.16 kg/190 °C) gr/10 min (Granule) | 10 |
| ***ASTM D3418*** | Melting Point (DSC), min °C | 11 |
| ***ISO 527-1 and -2 or******ISO 527-1 and -3 or******ASTM D638*** | Elongation at break % min | 12 |
| ***ISO 527-1 and -2 or******ISO 527-1 and -3 or******ASTM D638*** | Tensile strength @ Yield 23±2 °C, min MPa | 13 |
| ***ISO 15512*** | Water content, max % | 14 |
| ***ISO 306 or ASTM D1525*** | VICAT Softening A/50 (9.8 N) min °C | 15 |
| ***Poly Ethylene*** |
| ***ISO 1183 (all parts) or******ASTM D792 or******ASTM D1505*** | Density @ 23±2 °C gr/cm3 | 16 |
| ***ISO 3146 or******ISO 11357-1 and -3 or******ASTM D3418*** | Melting index (2.16 kg/190 °C) gr/10 min(Granule) | 17 |
| ***ISO 3146 or******ISO 11357-1 and -3 or******ASTM D3418*** | Melting index (2.16 kg/190 °C) gr/10 min, (Extruded) | 18 |
| ***ISO 527-1 and -2 or******ISO 527-1 and -3 or******ASTM D638*** | Elongation at break %, min | 19 |
| ***ISO 1133*** | Melting point (DSC), min , °C | 20 |
| ***ISO 527-1 and -2 or******ISO 527-1 and -3 or******ASTM D638*** | Tensile strength, at break 23±2°C, min, MPa | 21 |
| ***ISO 527-1 and -2 or******ISO 527-1 and -3 or******ASTM D638*** | Yield strength, at 23±2°C, min, MPa | 22 |
| ***ISO 868*** | Hardness Shore D min | 23 |
| ***ISO 15512*** | Water content , max % | 24 |
| ***ISO 11357*** | O.I.T @ 210 °C minute | 25 |
| ***ISO 306 or ASTM D1525*** | VICAT Softening temperature A/50(9.8 N ) min | 26 |
| ***ASTM D 1603*** | Carbon Black Content % | 27 |
| ***ISO 18553*** | Carbon black dispersion | 28 |
|  | Stress Cracking resistance(50 °C MEK , 1000 hr) | 29 |
| ***ISO 21809*** | Thermal Aging % | 30 |
| ***Coal Tar Enamel*** |
| ***BS 4147-Appendix B*** | Filler content by ignition, % by mass | 31 |
| ***BA 2000*** | Softening point (Ring and Ball), °C | 32 |
| ***BS 4147-Appendix D*** | Penetration@ 25 °C, 0,1 mm@ 45 °C, 0,1 mm | 33 |
| ***BS 4147-Appendix C*** | Density (gr/cm3) | 34 |
| ***BS 4147*** | Sag, maximum mm 80°C 24 h | 35 |
| ***BS 4147*** | @ 30 °C | Peel initial and delayed, maximum mm | 36 |
| @ 40 °C |
| @ 50 °C |
| 60 °C @ |
| ***ASTM G 8*** | Cathodic disbonding, disbonded radiusafter 28 d, maximum, mm | 37 |
| ***Bitumen & Modified Bitumen Enamel*** |
| ***BS 4147-Appendix B*** | Filler content by ignition, % by mass | 38 |
| ***BS 2000*** | Softening point (ring and ball), °C | 39 |
| ***BS 4147-Appendix D*** | Penetration at 25 °C, 0,1 mm | 40 |
| ***BS 4147-Appendix C*** | Density (gr/cm3) | 41 |
| ***BS 4689*** | Flash point (Cleveland open cup), minimum °C | 42 |
| ***BS 4147-Appendix E*** | Sag, maximum mm | 43 |
| ***BS 4147-Appendix G*** | Impact disbonded— Area, maximum mm2 | 44 |
| ***BS 4147-Appendix H*** | @ 30°C | Peel initial anddelayed, maximummm | 45 |
| @ 40 °C |
| @ 50 °C |
| 60°C @ |
| ***BS 4147-Appendix F*** | Bend at 0 °C, minimum, mm | 46 |
| ***ASTM G 8*** | Cathodic disbonding, disbonded radiusafter 28 d, maximum, mm | 47 |
| ***Outer Wrap*** |
| ***ASTM D 146*** | Thickness (mm) | 48 |
| ***ASTM D 146*** | Mass per area, minimum | 49 |
| ***ASTM D 882*** | Tensile strength, minimumLongitudinal (N/ 50 mm)Transverse (N/50 mm) | 50 |
| ***AWWA C 203*** | Weight Loss on Heating (% by weight) | 51 |
| ***ASTM D 737*** | Porosity | 52 |
| ***ASTM D 146*** | Pliability | 53 |
|  | Resistance to waterLongitudinal (N/ 50 mm)Transverse (N/50 mm) | 54 |
|  | Appearance | 55 |
| ***Inner Wrap*** |
| ***ASTM D 146*** | Thickness (mm) | 56 |
| ***ASTM D 146*** | Mass per area, minimum | 57 |
| ***ASTM D 882*** | Tensile strength, minimumLongitudinal (N/50 mm)Transverse (N/50 mm) | 58 |
| ***EN 10300*** | Resistance to OilLongitudinal (N/ 50 mm)Transverse (N/50 mm) | 59 |
| ***ASTM D 146*** | Pliability | 60 |
| ***EN 10300*** | Binder Content max | 61 |
| ***EN 10300*** | Appearance | 62 |
| ***Primer*** |
| ***EN ISO 2431*** | Flow time (Flow Cup No 4 @ 23 °C), seconds | 63 |
| ***EN ISO 13736*** | Flash point (Abel closed cup), minimum °C | 64 |
| ***EN 10300*** | Volatile matter, maximum % loss by mass | 65 |
| ***EN 10300*** | Ash Content(mass) Max%Loss by mass | 66 |
| ***Heat Shrinkable Sleeve Field Joint*** |
| ***ASTM D 1000*** | Backing thickness (as supplied) , min | 67 |
| ***ASTM D 1000*** | Adhesive thickness (as supplied), min | 68 |
| ***ASTM D 1000*** | Total thickness (as Supplied) , min | 69 |
| ***ASTM D 2240*** | Hardness @ 23 °C , Shore D min | 70 |
| ***EN 12068*** | Impact resistance at 23 °C , min ( J ) | 71 |
| ***EN 12068*** | Peel strength to pipe surface and to factory coating , min@ 23 °C N/mm@ 80 °C N/mm | 72 |
| ***ASTM E 28*** | Ring and ball softening point ofadhesive , min 0C | 75 |
| ***EN 12068*** | Lap shear strength to pipe surface and factory coating , min N/mm2@ 80 °C | 76 |
| ***ASTM D638*** | Ultimate Elongation , min % | 77 |
| ***EN 12068*** | Indentation resistance pressure (test condition)@ 80 °C N/mm2 | 78 |
| ***ASTM D638*** | Heat aging , 21 days at 100 °C , min- Elongation %-Peel Strength to pipe surface | 79 |
| ***ASTM D 2671*** | Heat shock , 4 hours at 225 °C | 80 |
| ***EN 12068*** | Ultraviolet irradiation resistanceratio of elongation at break | 81 |
| ***EN 12068*** | Cathodic disbondment resistance max@ 23 °C@ 80 °C | 82 |
| ***EN 12068*** | Specific electrical insulation resistance RS100. min | 83 |
| ***TP 206*** | Soil stress creep resistance, mm (max), 24 hours @ 80 ˚C | 84 |
| ***Hand Applied 2Ply Bituminous Joint Wrap*** |
| ***ASTM D 1000*** | Thickness (mm) | 101 |
| ***ASTM D 1000*** | Tensile strength (kg/cm) | 102 |
| ***ASTM D 1000*** | Elongation at break (%) | 103 |
| ***ASTM D 1000*** | Adhesion to primed steel (kg/cm) | 104 |
| ***ASTM D 1000*** | Adhesion to self (kg/cm) | 105 |
| ***ASTM D 1000*** | Dielectric strength(kv/mm) | 106 |
| ***EN 12068*** | Indentation resistance (n/mm2) | 107 |
| ***EN 12068******Annex H*** | Impact resistance at 23 °C (J) | 108 |
| ***ASTM D 570*** | Water absorption | 109 |
| ***ASTM G 8*** | Cathodic disbondment at 23°C(mm -Radius) | 110 |
| ***EN 12068******Annex J*** | Specific electrical insulation resistance RS 100,min | 111 |
| ***3Ply Co-Extruded Plastic Tape*** |
| ***ASTM D 1000*** | Thickness (mm) | 112 |
| ***ISO 527-1 and -2 or******ISO 527-1 and -3 or******ASTM D638*** | Tensile strength (N/cm) | 113 |
| ***ISO 527-1 and -2 or******ISO 527-1 and -3 or******ASTM D638*** | Elongation at break (%) | 114 |
| ***EN 12068******Annex C*** | Peel strength to primed steel (N/cm)@ 23°C@ 50 °C | 115 |
| ***EN 12068******Annex C*** | Peel strength tape to tape (kg/cm)@ 23°C@ 50°C | 116 |
| ***ASTM D 149*** | Dielectric strength (kv/mm) min | 117 |
| ***EN 12068******Annex J*** | Insulation resistance –Ohm.m2 | 118 |
| ***EN 12068******Annex H*** | Impact resistance at 23°C (J) | 119 |
| ***ASTM D 570*** | Water absorption Max | 120 |
| ***EN 12068*** | Lap shear strength@ 50 °C N/mm2, min | 121 |
| ***EN 12068******Annex K*** | Cathodic disbonding (mm -Radius)@ 23 °C@ 50 °C | 122 |
| ***EN 12068*** | Indentation resistance@ 50 °C , mm- Residual thickness- Holiday detection | 123 |
|  | Saponification value carrier film and Adhesive , mg KOH/g max | 124 |
| ***Outer wrap (white wrap)*** |
| ***ASTM D 1000*** | Thickness (mm) | 125 |
| ***ASTM D 1000*** | Tensile strength (N/mm) | 126 |
| ***ASTM D 1000*** | Elongation at break (%) | 127 |
| ***ASTM D 1000*** | Adhesion to self (@ over laps) (N/mm) | 128 |
| ***ASTM D 1000*** | Adhesion to Inner wrap (N/mm) | 129 |
| ***ASTM D 149*** | Dielectric strength (kv/mm)(In conjunction with inner layer) | 130 |
| ***EN 12068******Annex G*** | Indentation resistance (N/mm2) | 131 |
| ***EN 12068******Annex H*** | Impact resistance @ 23 °C (N.M)(In conjunction with inner layer) | 132 |
| ***ASTM D 570*** | Water absorption max | 133 |
| ***EN 12068*** | Heat aging in 30 days at 60 °CReduction of elongation and tensile strength | 134 |

**آزمون­های تخصصی پوشش های خطوط لوله­های مورد استفاده در صنایع آب آشامیدنی**

|  |
| --- |
| *Drinking Water Pipe line coatings*  |
| *ASTM D 1475* | Density @ 25°C | 1 |
| *AWWA C 210* | Immersion – Deionized Water | 2 |
| *AWWA C 210* | Immersion – 1 Wt.% Sulfuric Acid | 3 |
| *AWWA C 210* | Immersion – 1 Wt.% Sodium Hydroxide | 4 |
| *ASTM D 4752* | Rub Test | 5 |
| *ASTM D 2697* | Volume Weight Percent | 6 |
| *ASTM D 2369* | Solid Weight Percent | 7 |
| *ASTM D 562* | Krebs Viscosity @ 60°C | 8 |
| *ASTM D 1640* | Drying Time | 9 |
| *ASTM D 523* | Gloss | 10 |
|  | Pot Life @ 60°C | 11 |
| *ASTM D 4400* | Sagging Test | 12 |
| *AWWA C 210* | Cathodic Disbonding | 13 |
| *Drinking Water Contamination test* |
| *BS 6920* | Suitability of non-metallic products for use in contact with water | 14 |

**"برخی از تجهیزات"**

|  |  |
| --- | --- |
| Melt Flow Index (MFI) | Shore D- Hardness |
| http://www.santamco.com/Imager.ashx?id=319 | http://www.gotech.biz/gotech_admin/upload/2302171313481441038382.jpg |
| Cathodic Disbonding | **Tensile+200° C Oven (Peeling-LapShear)** |
| Image result for cathodic disbonding setup | http://www.santamco.com/Imager.ashx?id=52089 |
| Vicat Softening Point | **DSC** |
|  |  |
| Optical Microscopy |  **-40°C Freezer** |
|  | Image result for ‫فریزر ژال طب‬‎ |
| Softening point | **Penetration** |
| Z:\پژوهشکده پوششهای سطح و فناوریهای نوین\گروه پژوهشی روکش‌های سطح و خوردگی\دکتر یاری\PHOTO\Softening point.jpg | Z:\پژوهشکده پوششهای سطح و فناوریهای نوین\گروه پژوهشی روکش‌های سطح و خوردگی\دکتر یاری\PHOTO\penetration.jpg |
| Particle Size Analysis |
| Image result for malvern mastersizer 2000 |